## Slide 1: Cutting Tool Materials Eng R. L. Nkumbwa Copperbelt University 2010

## Slide 2: History of Cutting Tool Materials
Cutting tool used during the industrial revolution in 1800 A.D
First cutting tool was cast using crucible method (1740) and slight hardened by H.T.
1868: R. Mushet found by adding Tungsten we can increase hardness and tool life ( Air Quenching)

## Slide 3: History of Cutting tools
F.W.Taylor in Pennsylvania did the most basic research in metal cutting between 1880-1905
  Invented high speed steel (better H.T. process)
  Better alloy
Tungsten Carbide was first synthesized in 1890.
Took 3 decades before we got Cemented carbide
First used in Germany
Sintering technology was invented

## Slide 4: Cutting tool materials
Selection of cutting tool materials is very important
What properties should cutting tools have?
  Hardness at elevated temperatures
  Toughness so that impact forces on the tool can be taken
  Wear resistance
  Chemical stability

## Slide 5: Types of Tool Materials
Carbon + medium alloy steel
High Speed Steel (HSS)
Cast cobalt alloys
Carbides
Coated tools
Ceramics
Cubic boron nitride
  invented by GE in 1969
Silicon Nitride
Diamond

## Slide 6: High Speed Steel (HSS)
Early 1900s
Very highly used alloy steel
Can be hardened to various depths
Good wear resistance
High toughness
Good for positive rake angle tools.
Two basic types of HSS
  Molybdenum: ( M Series)
  Tungsten: (T Series)

## Slide 7: High Speed Steel
T Series
12 – 18 % Tungsten
Chromium, Vanadium etc.
M Series
  10% Molybdenum
  Chromium, Vanadium, Tungsten, Cobalt
  Better abrasion resistance
  Less expensive
  Less distortion
  95% of HSS used is M series

## Slide 8: High Speed Steel
Manufacturing
Cast
Powder Metallurgy
Applications
Taps
Gear cutters
Drills

## Slide 9: Cast Cobalt (Stellite Tool)
38 – 53% Cobalt
30 – 33% Chromium
10 – 20 % Tungsten
High hardness (58-64 HRC)
Good wear resistance
High temperature hardness
No Toughness
  not suitable for intermittent cutting
Good for deep boring, continuous turning
( better than HSS)

## Slide 10: Carbides
Most HSS and Cast Alloy have very low “high temperature” hardness
Low life for high speed machining
Carbides
  High temp Hardness
  Low thermal expansion
  High modulus of elasticity
Tungsten Carbide (W-C)
Used for cutting non ferrous abrasive and metal + cast iron
Tungsten Carbide particles are bonded in Cobalt matrix

## Slide 11
Cermet (Titanium Carbide)
Invented in 1950
Used since 1970
Coated Carbide
Made of WC – Co – TiC - TiN
3 – 4 coatings of Al2O3

## Slide 12
Particles sized 1- 5 mm are pressed and sintered into desired shapes (% of Co may vary)
W-C is also compounded, sometimes with Titanium and Tantalum to improve hot hardness and crater wear
Titanium Carbide
Ti-C has Ni-Mb matrix
Good wear resistance and poor toughness
Good for machining steel
Higher speed than W-C

## Slide 13
Stiffness of the machine is important
Low feed, low speed and chatter can cause failure
Carbide Inserts
Smaller angle has less strength
Coated tools
The coating is 5-10 mm in thickness
http://www.carbidedepot.com/bbars.asp

## Slide 14
Titanium Nitride
Low friction
High hardness
Resistance to high temperature
Improves life of HSS, carbides
Ceramics
High temperature resistance
Chemical inertness
Wear resistance
Al203

## Slide 15
Ceramic Cutting Tool
Brittle
Nowadays used extensively

## Slide 16
Ceramic
Fine grained , high purity Al203 cold pressed at high temperature and sintered at high temperature (white)
Cermets
70% Al203 30 % T-C
Very high temperature hardness
High abrasion resistance
More chemical stability
Less tendency for adhesion so less BUE
Good surface finish while machining steel and CI
Poor toughness for intermittent cutting

## Slide 17
Cubic Boron Nitride
Next to diamond, the hardest material
0.5-1mm polycrystalline cubic boron nitride
High wear resistance
But brittle
Used for machining hardened steel and high temperature alloys ( Ni for instance)

## Slide 18
Silicon Nitride
Used for super alloys
Diamond
Low friction and high wear resistance
Good cutting edge
Single crystal diamond are used to machine copper to a high surface finish
Because they are brittle rake angle has to be low

## Slide 19
Polycrystalline diamond tool
(Compacted) synthesized crystals
Fused at high temperatures and high pressures

## Slide 22
Tool life curves for various tool materials in medium and light turning operations as a function of cutting speed. Note how the curve for ceramics crosses over the curve for T-C as speed , hence temperature, increases
Effect of cobalt content in T-C tools over mechanical properties. Hardness is directly related to compressive strength and hence, inversely, with wear

## Slide 23
Relative time required to machine with various tool cutting materials, indicating the year the cutting tool material were first introduced

## Slide 24
Property | Carbon and low to medium alloy steels | HSS | Cast Cobalt alloys | Cemented carbide | Coated carbide | Ceramics | Poly -crystalline CBN | Diamond
Depth of cut | Light to medium | Light to heavy | Light to heavy | Light to heavy | Light to heavy | Light to heavy | Light to heavy | Very light for single crystal
Finish Obtainable | Rough | Rough | Rough | Good | Good | Very good | Very good | excellent
Method of processing | Wrought | Wrought, cast, HIP, sintering | Cast, HIP and sintering | Cold pressing and sintering | CVD | Cold pressing and sintering | High pressure and high temp. sintering | High pressure and high temp sintering
Fabrication | Machining and grinding | Machining and grinding | Grinding | Grinding | Grinding | Grinding | Grinding and polishing | Grinding and polishing

## Slide 25
Property | Carbon and low to medium alloy steels | HSS | Cast Cobalt alloys | Cemented carbide | Coated carbide | Ceramics | Poly -Crystalline CBN | Diamond
Hot hardness |  |  |  |  |  |  |  | 
Toughness |  |  |  |  |  |  |  | 
Wear resistance |  |  |  |  |  |  |  | 
Chipping resistance |  |  |  |  |  |  |  | 
Cutting speed |  |  |  |  |  |  |  | 
Thermal shock resistance |  |  |  |  |  |  |  | 
Total material cost |  |  |  |  |  |  |  | 
increasing
increasing
increasing
increasing
increasing
increasing
increasing